Typical Certification of Analysis

AISI TYPE

A2 GFS/GFO

This is to certify that the material described above meets the following chemistry limits.

| C | MN | S1 | P | S | CR | W | MO | V |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| .90 / 1.05 | .30 / .90 | .15 / .35 | .020 Max | .020 Max | 4.75 / 5.5 |  | .90 / 1.25 | .20 / .40 |

ASTM A-681

MERCURY FREE

Sworn to and subscribed before me on this the

Wednesday, July 29, 2026

Your Partner for Today’s Metal Needs