Typical Certification of Analysis

AISI TYPE

D2

This is to certify that the material described above meets the following chemistry limits.

| C | MN | S1 | P | S | CR | W | MO | V |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1.40 / 1.60 | .20/ .60 | .20 / .60 | .025 Max | .025 Max | 11.00 / 13.00 | ------- | .70/1.10 | .80 / 1.00 |

ASTMA 681

Sworn to and subscribed before me on this the

Thursday, August 11, 2016

Your Partner for Today’s Metal Needs