Typical Certification of Analysis

AISI TYPE

S7 GFS/GFO

This is to certify that the material described above meets the following chemistry limits.

| C | MN | S1 | P | S | CR | W | MO | V |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| .48 / .55 | .60 / .80 | .20 / .50 | .025 / MAX | .025 Max | 3.10 / 3.50 |  | 1.30 / 1.70 | .20 / .30 |

ASTM A-681

MERCURY FREE

Sworn to and subscribed before me on this the

Wednesday, July 29, 2026

Your Partner for Today’s Metal Needs