Typical Certification of Analysis

AISI TYPE

W1

This is to certify that the material described above meets the following chemistry limits.

| C | MN | S1 | P | S | CR | W | MO | V |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| .90 / 1.05 | .30 / .50 | .10 / .25 | .025 Max | .025 Max | .15 Max | .15 Max | .10 Max | .10 Max |

Sworn to and subscribed before me on this the

Thursday, August 11, 2016

Your Partner for Today’s Metal Needs